СЄ

Gleeson Precast Golden, Co Tipperary 13

IS EN 13242:2002+A1:2008 Aggregates for hydraulically bound and Unbound Materials 150mm Clean Stone

| Particle Shape FI21 |  |
| --- | --- |
| Particle Size |  |
| Particle Density | 2.60Mg/m3 |
| Fines Content | F2 |
| Resistance to fragmentation/crushing | LA21 |
| Resistance to polishing | PSV43 |
| Resistance to abrasion | AAV1.8 |
| Resistance to wear | Mde 15 |
| Composition/content |  |
| Chlorides | C <0.01% |
| Acid Soluble Sulphates | AS 0.1% |
| Total Sulphur | TS 0.1% |
| Volume Stability |  |
| Dry Shrinkage | 0.027% |
| Water Absorption | WA 0.3% |
| Emission of Radioactivity | NA |
| Release of heavy metals | NA |
| Release of polyacromatic hydrocarbons | NA |
| Release of any other dangerous substances | NA |